## Slide 1
SWAN (K18X001.00) Cross section Test Explain
Prepare: JBD-VN-ME
Date: 2022.Sep-05

## Slide 2
U1
1.1. Where is point start #1 ? :
ROW 1
ROW 2
ROW 3
1.2. Why chose the section Row 1, 2, 3 :
SWAN (K18X001.00) Cross Section
Row 1
1#
22#
1.3 If proceed Next section test, please analysis below in order :
U1313
ROW 1
ROW 2
ROW 3
ROW 4
Definition rule will be as below:
Together with PE & PQE department to discuss the choice of U1 & U1313 cutting position.
Next build, the experiment can be based on the customer's request to select the cutting position.
The positions of Row B, C, D can be done on request, but with positions A and A1 because
they are too close distance, so only 1 position cutting can be made.
Suggest customers choose another row cutting of position.

## Slide 3
SWAN (K18X001.00) Cross Section
2.1. Please polish more with finer sandpaper:
Test Equipment:
Experimental Flow test:
Microstructure Inspection:
50X
200X
100X
500X
It is difficult to distinguish between the IMC layer and the
solder layer because the image is not clear.
Normal inspection of process:
After cutting, staff will use microscope levels to inspect the PAD positions with values
of 100 X or 200 X depending on the size of the PAD
If there is no abnormality, the PAD positions will be randomly selected to take 500X
and measure the IMC value.
If there is an abnormality, we will use 500X magnification to check that PAD position and
measure then calculate the Crack % value of the PAD pin.
Solder Void
Traces of
Grinding & Polishing
Magnify 200X
Magnify 500X

## Slide 4
SWAN (K18X001.00) Cross Section
Crack image of Sample:
200X

## Slide 5
SWAN (K18X001.00) Cross Section
2.2. BGA U1 review (Red point):
After cutting and inspecting with 200X magnification, 100% of all there are no abnormalities, so use only 200X magnification,
do not use 500X for all normal locations as below:
Row-1
3#
5#

## Slide 6
SWAN (K18X001.00) Cross Section
2.2. BGA U1 review (Red point):
After cutting and inspecting with 200X magnification, 100% of all there are no abnormalities, so use only 200X magnification,
do not use 500X for all normal locations as below:
Row-2
Row-3
9#
7#

## Slide 7
SWAN (K18X001.00) Cross Section
2.3. QFN U1313 review:
Magnify*500x
IMC layer
Magnify*200x
Magnify*200x

## Slide 8
SWAN (K18X001.00) Cross Section
2.2. Define the Solder crack:
If checking and detecting solder crack, Fii side defines and evaluate the same method as the customer's method.

## Slide 9
Thank you.