## Slide 1
SWAN- SMT Profile Verify Review
JBD-VN-ME
2022/02/14

## Slide 2
96.1516T00-SMT profile to optimal
1.Reflow Profile optimal
Summary: Void Solder > 30% unable to improved 100%. Fii RD & ME will keep and monitor this issue.
Status | Mass Product Stencil 0.10 mm Solder Paste: KOKI S3X58-M500 |  | 
 | Fail Q'Ty | Total | Defect rate
Void solder >30% | 4 | 400 | 1.00%
Solder ball | 5 | 400 | 1.25%
O-ring not seal | 0 | 400 | 0.00%
Profile feature | Fii suggest | Result
Ramp-up rate (Tsmax to Tp) | 3°C/second max | 0.88~0.92
Preheat Time (150-180°C) (ts) | 60-120 seconds | 94~99
Soldering time(TL>217°C) (tL) | 50-90 seconds | 82~87
Peak Temperature (Tp) | (Suggest 240-250°C) | 245.0~246.3
Time within 5°C of actual peak temperature (tp) | 20-40 seconds | 26~28
Ramp-down rate (Tp to Tsmax) | 3°C/second max | -0.91 ~ -0.82
Status | Mass Product Stencil 0.10 mm Solder Paste: KOKI S3X58-M500 |  | 
 | Fail Q'Ty | Total | Defect rate
Void solder >30% | 3 | 400 | 0.75%
Solder ball | 5 | 400 | 1.25%
O-ring not seal | 0 | 400 | 0.00%
Profile feature | Fii suggest | Result
Ramp-up rate (Tsmax to Tp) | 3°C/second max | 0.80~0.89
Preheat Time (150-180°C) (ts) | 60-120 seconds | 90~96
Soldering time(TL>217°C) (tL) | 50-90 seconds | 71~76
Peak Temperature (Tp) | (Suggest 240-250°C) | 245.1~247.8
Time within 5°C of actual peak temperature (tp) | 20-40 seconds | 26~29
Ramp-down rate (Tp to Tsmax) | 3°C/second max | -1.15 ~ -0.92
Time-1
Time-2

## Slide 3
96.1516T00-SMT profile to optimal
2.Customer Profile suggest
3.Fii Profile verify & optimal
Profile feature | Fii suggest | Result
Ramp-up rate (Tsmax to Tp) | 3°C/second max | 0.94~0.98
Preheat Time (150-180°C) (ts) | 60-120 seconds | 88~96
Soldering time(TL>217°C) (tL) | 50-90 seconds | 88~90
Peak Temperature (Tp) | (Suggest 240-250°C) | 245.0~246.0
Time within 5°C of actual peak temperature (tp) | 20-40 seconds | 27~29
Ramp-down rate (Tp to Tsmax) | 3°C/second max | -1.05 ~ -0.86
Status | Mass Product Stencil 0.10 mm Solder Paste: KOKI S3X58-M500 |  | 
 | Fail Q'Ty | Total | Defect rate
Void solder >30% | 3 | 400 | 0.75%
Solder ball | 6 | 400 | 1.50%
O-ring not seal | 0 | 400 | 0.00%
Time-3
Summary: Void Solder > 30% unable to improved 100%. Fii RD & ME will keep and monitor this issue.
(Note: Some components cannot withstand temperatures exceeding 250 degrees when passing through the Reflow)
Vendor suggest profile for MIC