## Slide 1
K18X001.00- MIC Soldering issue
Listens to customers, Meet customer expectation
I. Description:
- On 11/19, Customer sent request to do verify improvement void solder of MIC parts:
Reduce the 217oC reflow time (50-90secs): Current 87 secs to 50~55 secs (About 30 secs)
Add flux on the microphone pad side (on material) and mount by hand
Firstly, FXC will modify the reflow profile as customer request.

## Slide 2
Listens to customers, Meet customer expectation
II. Reflow profile as customer’s request:
Reflow profile as attached file
Scan X-RAY 50pcs: Some MIC parts were defect:
+ Solder ball: 5/200 (2.5%)
+ Void solder: 5/200(2.5%)
+ O-ring not seal: 4/200 (2.0%)
Summary: Void solder maximum<35%
OP will VI by magnifier &remove solder ball at AOI-post
O-ring not seal: Need to verify testing program then repair
 Try to optimize reflow profile
K18X001.00- MIC Soldering issue

## Slide 3
Listens to customers, Meet customer expectation
III. FXC optimize reflow profile:
Reflow profile is followed as vendor ’suggestion
Scan X-RAY 50pcs: Some MIC parts were defect:
+ Solder ball: 5/200 (2.5%)
+ Void solder: 3/200 (1.5%)
+ O-ring not seal: 0/200 (0.0%)
Summary: Void solder maximum<35%
OP will VI by magnifier &remove solder ball at AOI-post
O-ring is better
COMPARING REFLOW PROFILE |  |  |  | 
Item | Profile feature | Vendor suggest | U6_4/MIC3 | U6_5/MIC4
1 | Ramp-up rate (Tsmax to Tp) | 3°C/second max | 0.88 | 0.82
2 | Preheat Time (150-200°C) (ts) | 60-180 seconds | 80 | 78
3 | Soldering time(TL>217°C) (tL) | 60-150 seconds | 84 | 85
4 | Peak Temperature (Tp) | <260°C ( Suggest 240-245°C) | 241.2 | 241.7
5 | Time within 5°C of actual peak temperature (tp) | 20-40 seconds | 25 | 26
6 | Ramp-down rate (Tp to Tsmax) | 6°C/second max | -0.79 | -0.87
K18X001.00- MIC Soldering issue

## Slide 4
Listens to customers, Meet customer expectation
Status | NPI stage (100pcs) |  |  | Customer's request Profile (50pcs) |  |  | FXC optimize profile (50pcs) |  | 
 | Fail Q'Ty (pcs) | Total | Defect rate | Fail Q'Ty (pcs) | Total | Defect rate | Fail Q'Ty (pcs) | Total | Defect rate
Void solder >30% | 11 | 400 | 2.75% | 5 | 200 | 2.50% | 3 | 200 | 1.50%
Solder ball | 17 | 400 | 4.25% | 5 | 200 | 2.50% | 5 | 200 | 2.50%
O-ring not seal | 0 | 400 | 0.00% | 4 | 200 | 2.00% | 0 | 200 | 0.00%
Summary:
- The solder ball rate seem be better a little but it is not improved completely.  Will modify stencil and verify new solder paste.
- Void solder is also better. The maximum void solder is not over 35%
- Reflow as customer’s request may affect to O-ring sealing
IV. Compare between reflow profiles:
V. Verify testing program:
3pcs defect ( total 4 positions) were tested on line.
Result: pass
K18X001.00- MIC Soldering issue