## Slide 1
SWAN (K18X001.00) Cross section Test overview
Prepare: JBD-VN-ME
Date: 2022.08.18

## Slide 2
1.PCBA Cross Section Map
U1
U1313
ROW 1
ROW 2
ROW 3
ROW1
ROW2
ROW3
ROW4
Based on the diagram and conduct cross section experiment with positions U1 & U1313.
A. Location of cross section experiment with PCBA:

## Slide 3
PCBA Comparison image of the cross section experiment with component.
B. Contrast image between Sample Pass and Fail:
1.PCBA Cross Section Map
Fail
Pass

## Slide 4
C. BGA (U1) &QFN (U1313) image-Magnify*500x
1.PCBA Cross Section Map
Checking the cross section position of the component did not find any abnormality

## Slide 5
2. PCBA Cross Section location images on locations
A. Location U1 (BGA)-Magnify*200x:
1# | 2# | 3# | 4# | 5# | 6# | 7# | 8# | 9# | 10# | 11#
12# | 13# | 14# | 15# | 16# | 17# | 18# | 19# | 20# | 21# | 22#
Row-1
Detailed image of cross section experiment at position U1 (BGA)-No Crack

## Slide 6
2. PCBA Cross Section location images on locations
A. Location U1 (BGA):
1# | 2# | 3# | 4# | 5# | 6# | 7# | 8#
9# | 10# | 11# | 12# | 13# | 14# | 15# | NA
Row-2
Detailed image of cross section experiment at position U1 (BGA)-No Crack

## Slide 7
2. PCBA Cross Section location images on locations
A. Location U1 (BGA):
1# | 2# | 3# | 4# | 5# | 6# | 7# | 8# | 9# | 10# | 11# | 12#
13# | 14# | 15# | 16# | 17# | 18# | 19# | 20# | 21# | 22# | 23# | NA
Row-3
Detailed image of cross section experiment at position U1 (BGA)-No Crack

## Slide 8
B. Location U1313 (QFN)- magnify*200x :
2. PCBA Cross Section location images on locations
Row-1 & Row-2
Row-1 | 1# | 2# | 3# | 4# | 5# | 6# | 7# | 8#
Row-2 | 1# | 2# | 3# | 4# | 5# | 6# | 7# | 8#
Detailed image of cross section experiment at position U1313 (QFN)-No crack

## Slide 9
B. Location U1313 (QFN):
2. PCBA Cross Section location images on locations
Row-3 & Row-4
Row-3 | 1# | 2# | 3# | 4# | 5# | 6# | 7# | 8#
Row-4 | 1# | 2# | 3# | 4# | 5# | 6# | 7# | 8#
Detailed image of cross section experiment at position U1313 (QFN)-No crack

## Slide 10
Thank you.