## Slide 1
M2.5*7mm spec:
Material : carbon steel C-1018
Finish:Black ZN coating
Salt spray test:24H

## Slide 2
M2.5*7mm Screw to fix the heat spreader of soc top(4pcs)
Screw nut spec
Will apply Mechanical_thread_M2.5x0.45 screw.

## Slide 3
M3*10mm spec :
Material : carbon steel C-1018
Finish:Black ZN coating
Salt spray test:24H

## Slide 4
Will apply M3*10mm screw(4pcs) to fix the AMP board

## Slide 5
Will apply M3*10mm screw(5pcs) to fix the heatsperader AMP bottom