## Slide 1
BFX-UA300 model’s CPU Delaminated
PE : Nam
2022/11/17

## Slide 2
Problems description
#1
Fii encountered this symptom for the first time.
According to the image of the report, this component is suspected of delamination.
Here are a few possible causes of delamination component:
  Factory received PCBA from RD, maybe the process of transporting PCBA from RD to the factory too long makes CPU being sensitive to moisture  During component swapping used high temperatures, leading to delamination of CPU.
  Moisture sensitive components issue can come from anywhere.
VI of Factory | C-Scan image of Vendor
There was some scratches on the surface but didn’t cracked
SoC delaminated
SoC OK