## Slide 1
FOXCONN CPEG JBD_VN
Mar-30-2021
BFX-AT100 LED issue 8D report

## Slide 2
D1. Establish the Team
PM: Ben Zheng, Lam Zhou
PD: Ruan Wen Yong
QA: Rachel Nguyen, Robert Wu
SQE: Chun Ke
IE: Hai Ly
OTT:
  QA Manager :
Foxconn
  MFG Manager : David Yin
  QA Manager : Charlie Su/ CB Lin
Team Leader
Team Member

## Slide 3
D2. Description of Problems
Issue Description
Feb-2021, ALT customer complain LED ( Yellow & Purple ) issue on RMA center:
20-Fed-2021, Everlight received from Fii 7 pcs LED issue ( Yellow & Purple) for analysis root cause and Fii retained 1 pc for analysis. The detailed information is as below:
Type | SN | Production_Time | Vendor(Everlight) Lot Code | Vendor(Everlight) Date Code
Yellow | 2149688001201904040599 | 09/18/2019 15:50:01 | Y190730S1002DF | 190730
 | 2149688001201904024318 | 09/16/2019 05:40:20 | Y190730S1002DF | 190730
 | 2149688001201904032610 | 09/15/2019 16:02:53 | Y190730S1002DF | 190730
 | 2149688001201904017454 | 09/12/2019 08:20:13 | Y190730S1002DF | 190730
Purple | 2149688001201909023362 | 11/06/2019 16:21:41 | Y190914G1001DDFWX35 | 190914
 | 2149688001201908031823 | 10/12/2019 16:14:21 | LY190817S1002DDFWX35 | D190817
 | 2149688001201904035168 | 09/17/2019 03:01:02 | Y190730S1002DF | 190730
 | 2149688001201904041675 | 09/19/2019 03:15:47 | Y190730S1002DF | 190730

## Slide 4
Check production data and shipping data
Production data : 8 Units no have rework or repair data, all doing follow normal process:
Inspection at FT: Check LED color following SOP/ Quality alert and use golden sample for comparison.
D3. Containment
TT | SN | Production_Time | Invoice_No | Shipping_Time
1 | 2149688001201908031823 | 10/12/2019 16:14:21 | 5028016106 | 10/17/2019 3:38:10 PM
2 | 2149688001201909023362 | 11/06/2019 16:21:41 | 5028016338 | 11/8/2019 8:07:30 PM
3 | 2149688001201904017454 | 09/12/2019 08:20:13 | 5028015723 | 9/12/2019 1:44:15 PM
4 | 2149688001201904024318 | 09/16/2019 05:40:20 | 5028015801 | 9/18/2019 4:00:13 PM
5 | 2149688001201904035168 | 09/17/2019 03:01:02 | 5028015801 | 9/18/2019 4:00:13 PM
6 | 2149688001201904040599 | 09/18/2019 15:50:01 | 5028015800 | 9/18/2019 4:15:54 PM
7 | 2149688001201904032610 | 09/15/2019 16:02:53 | 5028015802 | 9/19/2019 5:04:34 AM
8 | 2149688001201904041675 | 09/19/2019 03:15:47 | 5028015802 | 9/19/2019 5:04:34 AM

## Slide 5
Check all LED Material in Warehouse with 123.00701.005 – 26-Mar-2021 .
D3. Containment
Result : Check 60K material ( 123.00701.005 ) Everlight vendor in warehouse , All is DC 202101 and 202102. No DC 190730, 190914, 190817 Led issue.

## Slide 6
FA report 7 pcs NG sample analysis
D4. Root Cause ( Everlight FA)

## Slide 7
D4. Root Cause
Ag migration explanation

## Slide 8
D5. Corrective Action ( Everlight vendor action)
Everlight will evaluate the solution of changing the bottom solid crystal adhesive into insulating adhesive.
The schedule from Everlight is as follows:
-Issue trial production order/material requisition-3/30
-The trial production of the project was completed-4/9
-Send samples to Fii-4/10
-Provide project trial production report-4/15
-Reliability Analysis Report-5/28
-Customer approve to introduce -6/4
-The 1st lot of new part ETD Everlight factory- 7/17
-Fii introduces into August production

## Slide 9
D6. Verification of effectiveness
SOP check LED on Test Function |  |  |  | 
FT1 Test Station | FT Test Station | RC Test Station | OBA Test Station | Quality Alert
Quality alert and SOP were already updated inspection requirement and hang on production line, IPQC keep audit and verifying the implementation on production line.

## Slide 10
D7. Prevent recurrence
Line leader remind all operators before production and monitor their operating daily.
IPQC will random sample check all test station and OBA station follow AQL .
Owner: PD/PQE: Huu Loi, Luu Mien